Cyclone Series Device

Thermal Resistance

May 2008, version 3.0                                                                                                                       Data Sheet

Revision

History

The following table shows the revision history for this data sheet.

| Tables 1 through 6 in this data sheet provide θ JA (junction-to-ambient thermal resistance) and θ JC (junction-to-case thermal resistance) values for Altera® Cyclone® series devices available in Ball-Grid Array (BGA), FineLine® BGA (FBGA), Micro FineLine BGA® (MBGA), Ultra FineLine BGA (UBGA), Pin-Grid Array (PGA), Plastic J-Lead Chip Carrier (PLCC), Plastic Enhanced Quad Flat Pack (EQFP), Thin Quad Flat Pack (TQFP), Plastic Quad Flat Pack (PQFP), and Power Quad Flat Pack (RQFP). Date | Document Version | Changes Made |
| --- | --- | --- |
| May 2008 | 3.0 | Updated Tables 2, 4, and 5. |
| July 2007 | 2.2 | Updated values for EP3C25 (E144) device in Table 2. |
| May 2007 | 2.1 | Updated values for EP3C10 (E144) device in Table 2 and added Revision History. |
| March 2007 | 2.0 | Added Cyclone III information. |
| April 2006 | 1.0 | Initial release. |

f For additional packaging information, refer to the Altera Device Packaging

Data Sheet.

Altera Corporation                                                                                                                                                1

DS-CYTHRML-3.0

Altera Device Package Information Data Sheet

Cyclone III Devices

| Thermal resistance values for Cyclone III devices are provided for a board meeting JEDEC specifications and for a typical board. The JEDEC board specifications require two signals and two power/ground planes and are available at www.jedec.org. The values are described in Tables 1 Table 1. Thermal Resistance Values for Cyclone III Devices |  |
| --- | --- |
| Value | Description |
| θJA (C/W) Still Air | Junction-to-ambient thermal resistance (θJA) with no airflow when a heat sink is not being used. |
| θJA (C/W) 100 ft./minute | Junction-to-ambient thermal resistance with 100 ft./minute airflow when a heat sink is not being used. |
| θJA (C/W) 200 ft./minute | Junction-to-ambient thermal resistance with 200 ft./minute airflow when a heat sink is not being used. |
| θJA (C/W) 400 ft./minute | Junction-to-ambient thermal resistance with 400 ft./minute airflow when a heat sink is not being used. |
| θJC (C/W) | Junction-to-case thermal resistance (θJC) for device. |
| θJB (C/W) | Junction-to-board thermal resistance (θJB) for specific board being used. |

through 4.

Table 2 provides θJA (junction-to-ambient thermal resistance) values and θJC (junction-to-case thermal resistance) values for Cyclone III devices on a board meeting JEDEC specifications for thermal resistance calculation.

| Table 2. Thermal Resistance of Cyclone III Devices for Board Meeting JEDEC Specifications (Part 1 of 2) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Device | Package | θJA (°C/W) Still Air | θJA (°C/W) 100 ft./min. | θJA (°C/W) 200 ft./min. | θJA (°C/W) 400 ft./min. | θJC (°C/W) |
| EP3C5 | E144 | 20 | 17.5 | 15.4 | 14 | 8.4 |
|  | F256 | 32.4 | 28.9 | 27 | 25.5 | 11.7 |
|  | U256 | 32.5 | 29.1 | 27.2 | 25.6 | 12.2 |
|  | M164 | 38.2 | 31.5 | 29.6 | 27.9 | 11.6 |
| EP3C10 | E144 | 20 | 17.5 | 15.4 | 14 | 8.4 |
|  | F256 | 32.4 | 28.9 | 27 | 25.5 | 11.7 |
|  | U256 | 32.5 | 29.1 | 27.2 | 25.6 | 12.2 |
|  | M164 | 38.2 | 31.5 | 29.6 | 27.9 | 11.6 |

2                                                                DS-CYTHRML-3.0                                                 Altera Corporation

Altera Device Package Information Data Sheet

| Table 2. Thermal Resistance of Cyclone III Devices for Board Meeting JEDEC Specifications (Part 2 of 2) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Device | Package | θJA (°C/W) Still Air | θJA (°C/W) 100 ft./min. | θJA (°C/W) 200 ft./min. | θJA (°C/W) 400 ft./min. | θJC (°C/W) |
| EP3C16 | E144 | 20 | 17.5 | 15.4 | 14 | 8 |
|  | Q240 | 27.2 | 24.7 | 22.1 | 17.8 | 4.3 |
|  | F256 | 28.5 | 25.1 | 23.2 | 21.7 | 9.1 |
|  | U256 | 28.8 | 25.4 | 23.5 | 22 | 9.7 |
|  | U484 | 26.9 | 23.5 | 21.6 | 20.1 | 8.5 |
|  | F484 | 22.9 | 19.4 | 17.7 | 16.2 | 6.9 |
|  | M164 | 34.7 | 28 | 26.1 | 24.4 | 9.2 |
| EP3C25 | E144 | 20 | 17.5 | 15.4 | 14 | 7.8 |
|  | Q240 | 27 | 24.5 | 21.8 | 17.6 | 4.2 |
|  | F256 | 27.5 | 24.1 | 22.2 | 20.7 | 8.5 |
|  | U256 | 27.9 | 24.5 | 22.6 | 21.1 | 9.1 |
|  | F324 | 26.6 | 23.1 | 21.3 | 19.8 | 8 |
| EP3C40 | Q240 | 25.8 | 23.2 | 20.6 | 17 | 4 |
|  | F324 | 23.2 | 19.7 | 18 | 16.5 | 5.9 |
|  | U484 | 22.8 | 19.3 | 17.6 | 16.1 | 5.9 |
|  | F484 | 19.8 | 16.3 | 14.6 | 13.2 | 4.8 |
|  | F780 | 18.7 | 15.2 | 13.5 | 12.2 | 4.5 |
| EP3C55 | F484 | 21.6 | 18.2 | 16.4 | 15 | 5.1 |
|  | U484 | 18.9 | 15.4 | 13.8 | 12.2 | 4.2 |
|  | F780 | 17.8 | 14.4 | 12.7 | 11.4 | 3.9 |
| EP3C80 | U484 | 20.4 | 16.9 | 15.2 | 13.8 | 4.4 |
|  | F484 | 18 | 14.5 | 12.9 | 11.5 | 3.6 |
|  | F780 | 16.9 | 13.5 | 11.8 | 10.5 | 3.3 |
| EP3C120 | F484 | 17.1 | 13.7 | 12 | 10.7 | 3.1 |
|  | F780 | 16 | 12.6 | 11 | 9.7 | 2.8 |

Table 3 provides board dimension information for each package.

| Table 3. PCB Dimensions Notes (1), (2) (Part 1 of 2) |  |  |  |  |
| --- | --- | --- | --- | --- |
| 2.5 mm Thick | Signal Layers | Power/Ground Layers | Package Dimensions (mm) | Board Dimensions (mm) |
| F780 | 9 | 9 | 29 | 89 |
| F484 | 7 | 7 | 23 | 83 |

Altera Corporation                                  DS-CYTHRML-3.0                                                                               3

Altera Device Package Information Data Sheet

| Table 3. PCB Dimensions Notes (1), (2) (Part 2 of 2) |  |  |  |  |
| --- | --- | --- | --- | --- |
| 2.5 mm Thick | Signal Layers | Power/Ground Layers | Package Dimensions (mm) | Board Dimensions (mm) |
| U484 | 7 | 7 | 19 | 79 |
| F324 | 6 | 6 | 19 | 79 |
| F256 | 6 | 6 | 17 | 77 |
| U256 | 6 | 6 | 14 | 74 |

Notes to Table 3:

(1)    Power layer Cu thickness 35 um, Cu 90%

(2)    Signal layer Cu thickness 17 um, Cu 15%

Table 4 provides θJA values and θJB (junction-to-board thermal resistance)

values for Cyclone III devices on a typical board.

| Table 4. Thermal Resistance of Cyclone III Devices for Typical Board (Part 1 of 2) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Device | Package | θJA (°C/W) Still Air | θJA (°C/W) 100 ft./min. | θJA (°C/W) 200 ft./min. | θJA (°C/W) 400 ft./min. | θJB (°C/W) |
| EP3C5 | F256 | 32.2 | 27.9 | 25.5 | 23.6 | 17.3 |
|  | U256 | 32.7 | 28.2 | 25.7 | 23.7 | 16.3 |
| EP3C10 | F256 | 32.2 | 27.9 | 25.5 | 23.6 | 17.3 |
|  | U256 | 32.7 | 28.2 | 25.7 | 23.7 | 16.3 |
| EP3C16 | F256 | 28.4 | 24.2 | 21.8 | 20 | 13.5 |
|  | U256 | 29 | 24.6 | 22.2 | 20.2 | 12.7 |
|  | U484 | 26.3 | 22.1 | 19.9 | 18.1 | 12.4 |
|  | F484 | 22.5 | 18.5 | 16.4 | 14.8 | 9.8 |
| EP3C25 | F256 | 27.5 | 23.2 | 20.9 | 19.1 | 12.6 |
|  | U256 | 28.1 | 23.7 | 21.3 | 19.4 | 11.8 |
|  | F324 | 26.4 | 22.3 | 20.1 | 18.3 | 12.4 |
| EP3C40 | F324 | 23.1 | 19 | 16.9 | 15.1 | 9.2 |
|  | F484 | 22.3 | 18.2 | 16 | 14.3 | 8.5 |
|  | U484 | 19.4 | 15.4 | 13.5 | 11.9 | 6.8 |
|  | F780 | 17.6 | 13.9 | 12.1 | 10.7 | 6.7 |
| EP3C55 | U484 | 21.2 | 17.1 | 15 | 13.3 | 7.5 |
|  | F484 | 18.6 | 14.6 | 12.6 | 11.1 | 6 |
|  | F780 | 16.8 | 13.1 | 11.3 | 9.9 | 5.9 |

4                                                                DS-CYTHRML-3.0                                                 Altera Corporation

Altera Device Package Information Data Sheet

| Table 4. Thermal Resistance of Cyclone III Devices for Typical Board (Part 2 of 2) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Device | Package | θJA (°C/W) Still Air | θJA (°C/W) 100 ft./min. | θJA (°C/W) 200 ft./min. | θJA (°C/W) 400 ft./min. | θJB (°C/W) |
| EP3C80 | U484 | 20 | 15.9 | 13.8 | 12.1 | 6.3 |
|  | F484 | 17.7 | 13.7 | 11.8 | 10.3 | 5.2 |
|  | F780 | 15.9 | 12.2 | 10.5 | 9.1 | 5.1 |
| EP3C120 | F484 | 16.8 | 12.9 | 11 | 9.4 | 4.4 |
|  | F780 | 15.1 | 11.4 | 9.6 | 8.3 | 4.2 |

Cyclone II Devices

Table 5 provides θ JA (junction-to-ambient thermal resistance) and θ JC

(junction-to-case thermal resistance) values for Cyclone II devices.

| Table 5. Thermal Resistance of Cyclone II Devices |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Device | Package | θJA (°C/W) 0 ft./min. | θJA (°C/W) 100 ft./min. | θJA (°C/W) 200 ft./min. | θJA (°C/W) 400 ft./min. | θJC (°C/W) |
| EP2C5 | F256 | 30.2 | 26.1 | 23.6 | 21.7 | 8.7 |
|  | T144 | 31 | 29.3 | 27.9 | 25.5 | 10 |
|  | Q208 | 30.4 | 29.2 | 27.3 | 22.3 | 5.5 |
| EP2C8 | F256 | 27.0 | 23.0 | 20.5 | 18.5 | 7.1 |
|  | T144 | 29.8 | 28.3 | 26.9 | 24.9 | 9.9 |
|  | Q208 | 30.2 | 28.2 | 26.9 | 21.7 | 5.4 |
| EP2C20 | Q240 | 26.6 | 24.0 | 21.4 | 17.4 | 4.2 |
|  | F256 | 24.2 | 20.0 | 17.8 | 16.0 | 5.5 |
|  | F484 | 21.0 | 17.0 | 14.8 | 13.1 | 4.2 |
|  | T144 | 27.6 | 26.4 | 25.4 | 23.8 | 9.6 |
| EP2C35 | F484 | 19.4 | 15.4 | 13.3 | 11.7 | 3.3 |
|  | U484 | 20.6 | 16.6 | 14.5 | 12.8 | 5.0 |
|  | F672 | 18.6 | 14.6 | 12.6 | 11.1 | 3.1 |
| EP2C50 | F484 | 18.4 | 14.4 | 12.4 | 10.9 | 2.8 |
|  | U484 | 19.6 | 15.6 | 13.6 | 11.9 | 4.4 |
|  | F672 | 17.7 | 13.7 | 11.8 | 10.2 | 2.6 |
| EP2C70 | F672 | 16.9 | 13.0 | 11.1 | 9.7 | 2.2 |
|  | F896 | 16.3 | 11.9 | 10.5 | 9.1 | 2.1 |

Altera Corporation                                  DS-CYTHRML-3.0                                                                               5

Altera Device Package Information Data Sheet

Table 6 provides θ JA and θ JB (junction-to-board thermal resistance) values for Cyclone II devices on a typical board.

| Table 6. Thermal Resistance of Cyclone II Devices |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Device | Package | θJA (° C/W) Still Air | θJA (° C/W) 100 ft./min. | θJA (° C/W) 200 ft./min. | θJA (° C/W) 400 ft./min. | θJB (°C/W) |
| EP2C5 | F256 | 30.2 | 25.8 | 22.9 | 20.6 | 14.8 |
| EP2C8 | F256 | 27.9 | 23.2 | 20.5 | 18.4 | 12.3 |
| EP2C20 | F256 | 24.7 | 20.1 | 17.5 | 15.3 | 9.1 |
|  | F484 | 20.5 | 16.2 | 13.9 | 12.2 | 7.2 |
| EP2C35 | F484 | 18.8 | 14.5 | 12.3 | 10.6 | 5.7 |
|  | U484 | 20.0 | 15.5 | 13.2 | 11.3 | 5.3 |
| EP2C50 | F484 | 17.7 | 13.5 | 11.4 | 9.8 | 4.5 |
|  | U484 | 19.0 | 14.6 | 12.3 | 10.6 | 4.4 |
| EP2C35 | F672 | 17.4 | 13.3 | 11.3 | 9.8 | 5.5 |
| EP2C50 | F672 | 16.5 | 12.4 | 10.5 | 9.0 | 4.6 |
|  | F672 | 15.7 | 11.7 | 9.8 | 8.3 | 3.8 |
| EP2C70 | F896 | 14.6 | 10.7 | 8.9 | 7.6 | 3.7 |

Cyclone

Devices

Table 7 provides θ JA (junction-to-ambient thermal resistance) and θ JC

(junction-to-case thermal resistance) values for Cyclone devices.

| θJA Table 7. Thermal Resistance of Cyclone Devices (Part 1 of 2) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Device | Pin Count | Package | θJC (°C/W) | (°C/W) Still Air | θ (°C/W) 100 ft./min. | θ (°C/W) 200 ft./min. | θ (°C/W) 400 ft./min. |
| EP1C3 | 100 | TQFP | 11.0 | 37.5 | 35.4 | 33.4 | 29.8 |
|  | 144 | TQFP | 10.0 | 31.1 | 29.4 | 27.9 | 25.5 |
| EP1C6 | 144 | TQFP | 9.8 | 29.4 | 28.0 | 26.7 | 24.7 |
|  | 240 | PQFP | 4.3 | 27.2 | 24.7 | 22.1 | 17.8 |
|  | 256 | FBGA | 8.8 | 28.7 | 24.5 | 22.3 | 20.5 |
| EP1C12 | 240 | PQFP | 4.0 | 26.0 | 23.4 | 20.8 | 17.1 |
|  | 256 | FBGA | 6.6 | 24.3 | 20.2 | 18.1 | 16.4 |
|  | 324 | FBGA | 6.1 | 23.0 | 19.8 | 17.7 | 16.1 |

JA                     JA                     JA

6                                                                DS-CYTHRML-3.0                                                 Altera Corporation

Altera Device Package Information Data Sheet

| θJA Table 7. Thermal Resistance of Cyclone Devices (Part 2 of 2) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Device | Pin Count | Package | θJC (°C/W) | (°C/W) Still Air | θ (°C/W) 100 ft./min. | θ (°C/W) 200 ft./min. | θ (°C/W) 400 ft./min. |
| EP1C20 | 324 | FBGA | 5.0 | 21.0 | 17.7 | 15.6 | 14.1 |
|  | 400 | FBGA | 4.7 | 20.7 | 17.5 | 15.5 | 13.9 |

JA                     JA                     JA

101 Innovation Drive San Jose, CA 95134 www.altera.com

Copyright © 2008 Altera Corporation. All rights reserved. Altera, The Programmable Solutions Company, the stylized Altera logo,  specific  device  designations, and  all other  words  and  logos  that are  identified as trademarks and/or  service marks are, unless noted otherwise, the trademarks and service marks of Altera Corporation in the U.S. and other countries. All other product or service names are the property of their respective holders.   Altera products are protected under numerous U.S. and foreign patents and pending applications,  mask  work  rights,  and  copyrights.  Altera  warrants  performance  of  its

semiconductor products to current specifications in accordance with Altera’s standard warranty, but reserves the right to make changes to any products and services at any time without notice. Altera assumes no responsibility or liability arising out of the application or use of any information, product, or service described herein except as expressly agreed to in writing by Altera Corporation. Altera customers are advised to obtain the latest version of device specifications before relying on any published information and before placing orders for products or services.

Altera Corporation                                                                DS-CYTHRML-3.0                                                7