RELIABILITY REPORT FOR

DS1921G Dallas Semiconductor

4401 South Beltwood Parkway

Dallas, TX 75244-3292

Prepared by:

09/23/2004

Ken Wendel

Reliability Engineering Manager

Dallas Semiconductor

4401 South Beltwood Pkwy. Dallas, TX 75244-3292

Email : ken.wendel@dalsemi.com ph:  972-371-3726

fax: 972-371-6016 mbl: 214-435-6610

Conclusion:

The following qualification successfully meets the quality and reliability standards required of all Dallas

Semiconductor products and processes:

DS1921G

In addition, Dallas Semiconductor's continuous reliability monitor program ensures that all outgoing product will continue to meet Maxim's quality and reliability standards. The current status of the reliability monitor program can be viewed at http://www.maxim-ic.com/TechSupport /dsreliability.html.*

Module Description:

A description of this Module can be found in the product data sheet. You can find the product data sheet at http://dbserv.maxim-ic.com/l_datasheet3.cfm.*

Reliability Derating:

A module device consists of one or more IC's in a single, upward integrated, package. This package is assembled to include batteries, crystals, and other piece parts that make up the configuration of the Module.  Because of either the complexity of the package or the included piece parts, standard high temperature reliability testing is not possible.  Therefore, in order to determine the reliability of module products, the reliability of each of the piece parts is individually determined, then summed to determine the reliability of the integrated module product. If there are "n" significant components in the module then:

Fr (module) = Fr (1) + Fr (2) + Fr (3) + ..... + Fr (n) Fr (module) = Failure rate of module

Fr(n) = Failure rate of the nth component

Failure Rates are reported in FITs (Failures in Time) or MTTF (Mean Time To Failure). The FIT rate is related to MTTF by:

MTTF = 1/Fr

| NOTE: MTTF is frequently used interchangeably with MTBF. The calculated failure rate for this module/assembly is: Module Device: | Module Units: | Quantity: | Fails: | Ea: | MTTF (Yrs): |  | FITs: |
| --- | --- | --- | --- | --- | --- | --- | --- |
| BR1225 | 1 | 100 | 1 | 1.0 | 175984 |  | 0.6 |
| DS1921 | 1 | 2052 | 2 | 0.7 | 21998 |  | 5.2 |
| DS9503 | 1 | 152 | 0 | 0.8 | 47516 |  | 2.4 |
| Totals: |  |  |  |  | 13853 |  | 8.2 |

The parameters used to calculate the module failure rate are as follows

Cf:  60%	Tu:  25	°C

The reliability data follows. A the start of this data is the module assembly information. This is a description of the module. The next section is the detailed reliability data for each stress found in the qualification / monitor. If there are additional processes or assemblies used as part of this report, a description of each will follow which includes the respective reliability data for that process/

assembly.  The reliability data section includes the latest data available. Some of this data may be generic with other packages or products.

* Some proprietary products may be excepted from this requirement.

Assembly Information:

Assembly Site:	Dallas

Pin Count:	2

Package Type:	Puk Can F50 Rev B w/Bump

Body Size:	0

Mold Compound:	FP4323, Dexter Hysol

Lead Frame:	PCB; FR4

Lead Finsh:

Die Attach:	Underfill FP4527, Dexter Hysol

Bond Wire / Size:	 / Flammability:	UL 94-V0

Moisture Sensitivity

(JEDEC J-STD20A)

Date Code Range:

MECHANICAL LIFE

DESCRIPTION

0047	to

DATE CD CONDITION

0102

READPOINT

QTY   FAILS

FA#

| MECHANICAL SHOCK | 0047 200G, 1/2 SINE, 6 MS 30 CYS 50 0 0047 10g or 0.06", 5Hz-2KHz, X Y Z axis 9 HRS 50 0 0102 200G, 1/2 SINE, 6 MS 30 CYS 50 0 0102 10g or 0.06", 5Hz-2KHz, X Y Z axis 9 HRS 50 0 Total: 0 |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| VIBRATION, VARIABLE FREQUENCY |  |  |  |  |  |
| MECHANICAL SHOCK |  |  |  |  |  |
| VIBRATION, VARIABLE FREQUENCY |  |  |  |  |  |
| STORAGE LIFE |  |  |  |  |  |
| DESCRIPTION | DATE CD CONDITION | READPOINT | QTY | FAILS | FA# |
| STORAGE LIFE | 0047 85 C | 1000 HRS | 77 | 0 |  |
| STORAGE LIFE | 0102 85 C | 1000 HRS | 77 | 0 |  |
|  |  | Total: |  | 0 |  |

TEMPERATURE CYCLE

DESCRIPTION

DATE CD CONDITION

READPOINT

QTY   FAILS

FA#

| TEMP CYCLE | 0047 | -40 TO 85C | 1000 | CYS | 77 | 0 |
| --- | --- | --- | --- | --- | --- | --- |
| TEMP CYCLE | 0102 | 0C TO 70C | 1000 | CYS | 77 | 0 |
| TEMP CYCLE | 0102 | -40 TO 85C | 1000 | CYS | 77 | 0 |
|  |  |  |  | Total: |  | 0 |

UNBIASED MOISTURE RESISTANCE

DESCRIPTION

DATE CD CONDITION

READPOINT

QTY   FAILS

FA#

| MOISTURE SOAK | 0047 | 60C/90% R.H. | 960 HRS | 77 | 0 |
| --- | --- | --- | --- | --- | --- |
| MOISTURE SOAK | 0102 | 60C/90% R.H. | 960 HRS | 77 | 0 |
|  |  |  | Total: |  | 0 |

Assembly Information:

Assembly Site:	Dallas

Pin Count:	2

Package Type:	Puk Can F50 Rev B w/Bump & overmold lid

Body Size:	0

Mold Compound:	?

Lead Frame:	PCB; FR4

Lead Finsh:

Die Attach:	Underfill FP4527, Dexter Hysol

Bond Wire / Size:	 / Flammability:	UL 94-V0

Moisture Sensitivity

(JEDEC J-STD20A)

Date Code Range:

0344	to

0344

ELECTRICAL CHARACTERIZATION

DESCRIPTION

DATE CD CONDITION

READPOINT

QTY   FAILS

FA#

| ESD SENSITIVITY | 0344 | IEC 1000-4-2 CONTACT 2000 VOLTS | 10 | PUL'S | 3 | 0 |
| --- | --- | --- | --- | --- | --- | --- |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 CONTACT 4000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 CONTACT 6000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 CONTACT 8000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 2000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 4000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 8000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 15000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 20000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 CONTACT 2000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 CONTACT 4000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 CONTACT 6000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 CONTACT 8000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 2000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 4000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 8000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 15000 VOLTS | 10 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0344 | IEC 1000-4-2 AIR 20000 VOLTS | 10 | PUL'S | 3 | 0 |
|  |  |  |  | Total: |  | 0 |