RELIABILITY REPORT FOR

DS2740, Rev A1

Dallas Semiconductor

4401 South Beltwood Parkway

Dallas, TX 75244-3292

Prepared by:

04/21/03

Ken Wendel

Reliability Engineering Manager

Dallas Semiconductor

4401 South Beltwood Pkwy. Dallas, TX 75244-3292

Email : ken.wendel@dalsemi.com ph:  972-371-3726

fax: 972-371-6016 mbl: 214-435-6610

Conclusion:

The following qualification successfully meets the quality and reliability standards required of all Dallas

Semiconductor products and processes:

DS2740, Rev A1

In addition, Dallas Semiconductor's continuous reliability monitor program ensures that all outgoing product will continue to meet Maxim's quality and reliability standards. The current status of the reliability monitor program can be viewed at http://www.maxim-ic.com/TechSupport /dsreliability.html.

Device Description:

A description of this device can be found in the product data sheet. You can find the product data sheet at http://dbserv.maxim-ic.com/l_datasheet3.cfm.

Reliability Derating:

The Arrhenius model will be used to determine the acceleration factor for failure mechanisms that are temperature accelerated.

AfT = exp((Ea/k)*(1/Tu - 1/Ts)) = tu/ts

AfT = Acceleration factor due to Temperature tu = Time at use temperature (e.g. 55°C)

ts = Time at stress temperature (e.g. 125°C)

k = Boltzmann’s Constant (8.617 x 10-5 eV/°K) Tu = Temperature at Use (°K)

Ts = Temperature at Stress (°K)

Ea = Activation Energy (e.g. 0.7 ev)

The activation energy of the failure mechanism is derived from either internal studies or industry accepted standards, or activation energy of 0.7ev will be used whenever actual failure mechanisms or their activation energies are unknown. All deratings will be done from the stress ambient temperature to the use ambient temperature.

An exponential model will be used to determine the acceleration factor for failure mechanisms, which are voltage accelerated.

AfV = exp(B*(Vs - Vu))

AfV = Acceleration factor due to Voltage

Vs = Stress Voltage (e.g. 7.0 volts)

Vu = Maximum Operating Voltage (e.g. 5.5 volts)

B = Constant related to failure mechanism type (e.g. 1.0, 2.4, 2.7, etc.)

The Constant, B, related to the failure mechanism is derived from either internal studies or industry accepted standards, or a B of 1.0 will be used whenever actual failure mechanisms or their B are unknown. All deratings will be done from the stress voltage to the maximum operating voltage. Failure rate data from the operating life test is reported using a Chi-Squared statistical model at the

60% or 90% confidence level (Cf).

The failure rate, Fr, is related to the acceleration during life test by:

Fr = X/(ts * AfV * AfT * N * 2)

X = Chi-Sq statistical upper limit

N = Life test sample size

Failure Rates are reported in FITs (Failures in Time) or MTTF (Mean Time To Failure). The FIT

rate is related to MTTF by:

MTTF = 1/Fr

NOTE: MTTF is frequently used interchangeably with MTBF.

The calculated failure rate for this device/process is:

FAILURE RATE:

MTTF (YRS):  1015

FITS:	112.4

The parameters used to calculate this failure rate are as follows:

Cf:  60%	Ea:  0.7	B:  0	Tu:  25	°C

Vu:  5.5

Volts

The reliability data follows. A the start of this data is the device information. This is a description of the device either used as a reliability test vehicle for a process / assembly qualification / monitor or a device used as part of a product qualification / monitor. Following this is the assembly information. This section includes a description of the assembly vehicle used to generate this reliability data for both qualifications and monitors. The next section is the detailed reliability data for each stress found in the qualification / monitor. If there are additional processes or assemblies used as part of this report, a description of each will follow which includes the respective reliability data for that process/ assembly. The reliability data section includes the latest data available.

Device Information:

Device:	DS2740

Process:	D6W-2P2M,HPVt,E2,EPROGVt,TCN1 ALOCOS:GOI Passivation:	Passivation w/Nov TEOS Oxide-Nitride

Die Size:	62 x 87

Number of Transistors:	7500

Interconnect:	Aluminum / 1% Silicon / 0.5% Copper

Gate Oxide Thickness:	150 Å

Assembly Information:

Qualification Vehicle:	DS2740

Assembly Site:	Carsem

Pin Count:	8

Package Type:	uSOP Body Size:	3x0.85

Mold Compound:	Nitto MP7400

Lead Frame:	Stamped Copper CDA194

Lead Finsh:	SnPb Plate

Die Attach:	84-1 LMISR4 Epoxy Silverfilled Ablebond

Bond Wire / Size:	Au / 1.3 mil

Flammability:	UL 94-V0

Moisture Sensitivity

(JEDEC J-STD20A)

Date Code Range:

Level 1

0305	to

0305

ELECTRICAL CHARACTERIZATION

DESCRIPTION

DATE CODE CONDITION

READPOINT

QUANTITY	FAILS

| ESD SENSITIVITY | 0305 | EOS/ESD S5.1 HBM 500 VOLTS | 1 | PUL'S | 3 | 0 |
| --- | --- | --- | --- | --- | --- | --- |
| ESD SENSITIVITY | 0305 | EOS/ESD S5.1 HBM 1000 VOLTS | 1 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0305 | EOS/ESD S5.1 HBM 2000 VOLTS | 1 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0305 | EOS/ESD S5.1 HBM 4000 VOLTS | 1 | PUL'S | 3 | 0 |
| ESD SENSITIVITY | 0305 | EOS/ESD S5.1 HBM 8000 VOLTS | 1 | PUL'S | 3 | 3 |
| LATCH-UP | 0305 | JESD78, I-TEST 125C | 2 | DYS | 6 | 0 |
| LATCH-UP | 0305 | JESD78, Vsupply TEST 125C | 2 | DYS | 6 | 0 |

Total:	3

OPERATING LIFE

DESCRIPTION

DATE CODE CONDITION

READPOINT

QUANTITY	FAILS

HIGH VOLTAGE LIFE

0305

125C, 6.0 VOLTS

192

HRS

Total:

45	0

0

STORAGE LIFE

DESCRIPTION

DATE CODE CONDITION

READPOINT

QUANTITY	FAILS

STORAGE LIFE

FAILURE RATE:

0305

150C

MTTF (YRS):  1015

192

FITS:	112.4

HRS

Total:

77	0

0